## Slide 1: Detection of B-Type Natriuretic Peptide (BNP) with Flexible Biosensors for Cardiovascular Risk Assessment
Seth So

## Slide 2: Sections
Key Concepts
  Biosensors, Principles, Sensing
Fabrication
  Processes & Materials, Process, PANI Synthesis, Final
Characterization
  Setup, Specificity and Sensitivity, Debye Screening, Hemolysis, Flexibility and Restoration
Testing and Analysis
  Human Serum, Healthy vs. Unhealthy, Data Classification
Future Work and Summary

## Slide 3: Key Concepts

## Slide 4: Biosensors
Biomolecule/Chemical Identification
  Surface Modification and Entrapment
  Antibody and Antigen Bindings
  Qualitative and Quantitative
Bioreceptor
Analyte
Transducer
Enzymes
Proteins
Antibodies
DNA
Optical
Mechanical
Electrical
Measurable Signal

## Slide 5: Working Elements
PANI Synthesis
  P-type semiconductor
  Chemical Polymerization
Surface Modification
  Crosslinkers
  Immunoassay Specificity
Conduction
  Amperometric/Conductometric
  Immunoassay Sensitivity

## Slide 6: Sensing mechanism
  Ion Sensitive Field Effect Transistor (ISFET)
  Solution acts as gate electrode
  [C] acts as gate voltage

## Slide 7: Fabrication

## Slide 8: Processes and Materials
Cleaning: Acetone, IPA, DI water, N2 gas
Photolithography: LOR-b, SC1827
Deposition: Chromium, Gold
PANI Synthesis: Aniline [C6H5NH2], APS [(NH4)2S2O8], Perchloric Acid [HClO4]
Surface Modification: EDC [C8H17N3], NHS [C4H5NO3], BSA, 0.01x PBS, Mouse BNP mAb, Recombinant Human BNP

## Slide 9: Device Fabrication Process
PET
LOR
Gold
Photoresist
PANI
Flexible substrate
Electrodes
Sensing material

## Slide 10: PANI Synthesis
Substrate
Ice bath (0~5ºC)
Step 1
pH ~ 7
Aniline
APS (oxidant)
Ice bath (0~5ºC)
Step 2
pH < 1
Aniline + APS
HClO4 (protonization)
+
+
1. Nucleation sites form on submerged substrate
2. Polymerization begins with protonization of oxidant
3. Reaction is complete after ~90minutes.

## Slide 11: CAD to Physical
Lithography and Deposition
Lithography and Chemical Synthesis
Surface Modification and BSA Blocking
PET substrate is flexible, sturdy, and chemically stable
Gold contacts and electrodes are highly conductive and biocompatible
Surface is modified with anti-BNP for 16 hours and blocked with BSA
PANI is chemically synthesized across the electrodes to act as P-type semiconductor
Notes:   Useful in Prognosis
    Poor prognosis typically consistent with higher blood concentrations
Normal concentration: <100pg/mL, grey 100-800pg/mL, high 1000pg/mL

## Slide 12: Characterization

## Slide 13
Potentiostat
Test circuit
Syringe pump
Multiple inlets
Gate power
supply
Data Acquisition
User Interface
Biosensor Chip
Biosensor Test System

## Slide 14: Data Representation
Voltage Sweep – from 0V – 0.4V
Legend – variable concentrations and samples
Current Response – magnitude directly proportional with [C]
Purpose of Test – includes types of samples

## Slide 15: Specificity and Sensitivity
  BNP showed the strongest electrical response out of the cardiac biomarkers
  Device displayed wide range of sensitivity
  Linear and Saturation regions

## Slide 16: Debye Screening Length
Larger Debye length (7.3nm)
Smaller Debye length (2.3nm)

## Slide 17: Effect of Hemolysis
  HGb reconstituted from lyophilized powder
  Δ 4pA from lowest to highest concentration
  Negligible effect in nanoampere regime
  Proposed mechanism: Nonpolar molecules solvate Fe ions

## Slide 18: Flexibility and Restoration
  None to highest flex resulted in ~10% amperage increase
  X5 flex (1cm-5cm) resulted in ~5% amperage increase
  Nearly complete restoration
  Consistent patterning and linear effect

## Slide 19: Testing and Analysis

## Slide 20: BNP in Healthy Individuals
  10 samples x 10 devices x 80 measurements
  Healthy [C] < 250pg, Unhealthy [C] > 800pg
  Average 0.85nA range across 10 devices

## Slide 21: Comparison of BNP Levels
Healthy vs. Unhealthy
  Signal response separate at 0.25V
  Higher variation at higher concentrations
  Clear delineation between healthy and unhealthy

## Slide 22: Data Classification
Artificial Intelligence
Machine Learning
Deep Learning
  A.I. – a program that can both sense and react autonomously
  M.L. – statistical algorithms and classifiers that improve with increased data exposure
  D.L. – subset of M.L. that uses layered neural network to process data
  M.L. to develop a health classifier with high predictive power
  Determine At-Risk percentage of cardiac failure
  Supplement sensor data with demographics information

## Slide 23: Machine Learning Analysis
  Training set size n=15
  Power – 96.4%, Accuracy – 95.2%
  Statistical principal components, limited dimensionality

## Slide 24: Future Work and Summary

## Slide 25: Future work
Continue BNP characterization
  Explore other biomarkers
Refine machine learning algorithm
  Increase dimensionality
Create integrated circuit
  Fabricate OLED’s on same chip
  Qualitative and quantitative data

## Slide 26: Future work - OLED Fabrication
  Fabricated
  Developed Recipe
  Generic Form
  Optimizing OLED turn on voltage and emissions
  Replace glass with PET
  Integrate OLED in series with biosensor

## Slide 27: Future work - OLED Integration

## Slide 28: Summary

## Slide 29: Detection of B-Type Natriuretic Peptide (BNP) with Flexible Biosensors for Cardiovascular Risk Assessment