## Slide 1: Finding Adhesion Energies of Graphene and MoS2 for Thermo-Electric Power Conversion Devices

## Slide 2: Sections
Key Concepts
  Thermo-Electric Power, Seebeck Effect, 2D materials
Experiment Set-up
  Sample Preparation, Calculations
Imaging
  SEM Location, AFM Imaging
Adhesion Energies
  Table Summary and Analysis
Conclusion and Future Work

## Slide 3: Key Concepts

## Slide 4: Thermo-Electric Power
Gradients
  Thermal: 2nd Law of Thermodynamics
  Electrical: potential and electrostatics
What happens if these are coupled?

## Slide 5: The Seebeck Effect
Thermoelectric Effect: Seebeck, Peltier, Thomson
Seebeck Effect
Generation of voltage via heat due to unequal electron energies, governed by Seebeck coefficient. Often utilized in thermopiles:

## Slide 6: 2D Materials
Definition: crystalline materials arranged into a single sheet of atoms.
Δz
Advantages: High SA:V  efficient conductivity (λ, σ)
Disadvantages: difficult integration, structurally less secure
Between MoS2 and Graphene, which has higher adhesion energy (γ) to metal substrates?

## Slide 7: Experiment Set-Up

## Slide 8: Sample Preparation
Prepare 2D material
Deposit nanoparticle (Au) onto metal substrate
Layer on 2D material
Sample ready for imaging
Copper growth substrate cleaned
2D material grown via CVD
PMMA spun on
Copper etched away
PMMA washed away
Test substrate cleaned
Nanoparticle deposited

## Slide 9: Calculations
4
Parameters of interest, a) top view b) side view
Assumptions:
Negligible deformation and contact area, small debonding angle, and spherical nanoparticle
Modeling:
Thin plastic membrane with centralized load, with simplifications:
γ = λEh() , λ=16

## Slide 10: Imaging

## Slide 11: SEM Location
SEM image of graphene on SiN with gold nanoparticles:
Working distance: 3.9mm, Magnification: 60.00kx, Operating Voltage: 10kV
Blister types:
Compound – clumping of multiple nanoparticles
Wrinkle – large infolding or crease of 2D material
Simple – target for most accurate modeling

## Slide 12: AFM imaging
Lot Statistics:
Graphene on:
MoS2 on:
SiO2: Pt:
Graphene: MoS2:
Average nanoparticle dimensions are comparable
Graphene variability possibly due to CVD process
Notes:   Useful in Prognosis
    Poor prognosis typically consistent with higher blood concentrations
Normal concentration: <100pg/mL, grey 100-800pg/mL, high 1000pg/mL

## Slide 13: Adhesion Energies

## Slide 14: Adhesion Energy Results
[Egrn = 1 TPa, EMoS2 = 0.33TPa]
Graphene shows overall stronger bonding
γ is not directly proportional to E
  Other surface effects such as Van der Waals have significant effect

## Slide 15: Conclusions and Future Work

## Slide 16: Conclusion & Future work
In this research, a test was conducted to determine which 2D material would have optimal binding to different metal substrates.
Graphene had better binding results than MoS2 across the board, especially for gold, which is the most polarizing substrate. This suggests that other surface forces have significant effects such as Van der Waals.
Future work involves further testing of different materials, device design and fabrication, and characterization.

## Slide 17: Acknowledgements
Special thanks to Dr. Yun and Jorge Torres, MCSI staff and organizers for the research opportunity.
Project funding came from:
ECCS1709307 and NSF HRD 1434012

## Slide 18: Questions?